## Slide 1
Materials Research Centre
Indian Institute of Science, Bangalore
Abhishek K. Singh
Indian Institute of Science, Bangalore
High throughput computational design of thermoelectric materials

## Slide 2: Acknowledgement
Indian Institute of Science, Bangalore
Theory and simulation group
Funding Agencies
NpMass, DST Nano Mission
Cray XC40 - "SahasraT"
Tej and Planck @MRC
Tribhuwan
George
SERC Team: Dr. Lakshmi, Vinod and Anup

## Slide 3
Recover waste heat
Introduction to thermoelectricity
Thermal gradient  Voltage difference
Seebeck effect
Peltier effect
Indian Institute of Science, Bangalore
http://edge.rit.edu/edge/P07440/public/Home

## Slide 4
It is relatively easy to reduce the thermal conductivity.
Increasing power factor at the same time is a challenging task.
Electronic thermal conductivity
Lattice thermal conductivity
Electrical conductivity
Thermopower
= dV/dT
Large power factor (PF)
Small lattice thermal conductivity
Challenges in efficient thermoelectric designing
How to identify a suitable semiconductor??
Indian Institute of Science, Bangalore

## Slide 5
Materials selection for thermoelectric
Large slope near the band edge results in high thermopower
Higher γ leads to higher ZT
M. G. Kanatzidis et al. Angew. Chem. 48, 8616 (2009)
Indian Institute of Science, Bangalore

## Slide 6
Materials with low thermal conductivity
PHYSICAL REVIEW B 85, 184303 (2012)
Indian Institute of Science, Bangalore
Materials with low lying flat acoustical branches
Low group velocity
Soft lattice
However soft lattice results into low melting point
Notes: As shown for PbTe its peculiar electronic structure results in high thermoelectric performance. However it is not the case always hence it is necessary to optimize the thermoelectric performance..

## Slide 7
Strategies for designing thermoelectric materials
Materials by “design” approach
Indian Institute of Science, Bangalore
Materials with high power factor and but low thermal conductivity
How can we scatter phonons but not electron
Phonon glass electron crystal
Breaking the inverse coupled dependence of S and σ
Special band structures, heavy light band mixtures
Tuning of carrier effective masses

## Slide 8
Materials with high power factor but low thermal conductivity
Indian Institute of Science, Bangalore

## Slide 9
Zintl materials
“Zintl phases” stand somewhere in-between metallic and ionic compounds
An electropositive cationic component (A) (alkali metal, alkali earth metal) and anionic component (X)
A
X
A
Complete charge transfer
Zintl-Klemm Concept
Indian Institute of Science, Bangalore

## Slide 10
Why this buzz about Zintl materials?
A2+ [Cd2Sb2]2-: A is electropositive and donates two electrons to the [Cd2Sb2] unit.
Cation
layer
Anion
layer
Nature Materials 7, 105 - 114 (2008)
Nature Materials 7, 105 - 114 (2008)
Phonon glass & electron crystal
Indian Institute of Science, Bangalore

## Slide 11
Electronic structure of Cd based Zintl compounds
Moderate gap semiconductor
Band structure exhibits mixed features
Suggests significant anisotropy in electrical conductivity
BaCd2Sb2
CdSb
CBM
VBM
System | Band gap (eV) |  |  | 
 | PBE | MBJ | MBJ+SOC | Exp
CdSb | 0.13 | 0.49 | 0.54 | 0.51
CaCd2Sb2 | 0.24 | 0.83 | 0.62 | 0.63
SrCd2Sb2 | Metal | 0.67 | 0.46 | x
BaCd2Sb2 | Metal | 0.57 | 0.37 | x
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)
Notes: The combination of heavy and light band results in pipe like Fermi surface at gamma-A direction indicative of better thermoelectric performance

## Slide 12
Transport properties
Huge anisotropy in electrical conductivity
Bipolar effect free large thermopower at 5 × 1018 cm−3 or higher carrier conc.
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)

## Slide 13
High power factor in Cd based Zintl compounds
T = 700 K
Large power factor resulting from co-existing high thermopower and electrical conductivity
Electron crystal
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)

## Slide 14
(W/mK)
Thermal conductivity
Thermal conductivity less than 1W/m-K at 600K
Ultra low thermal conductivity for BaCd2Sb2
Low phonon group velocity
Large Grüneisen parameter indicate strong anharmonicity in the lattice
Three phonon scattering influences the thermal conductivity most.
Phonon glass
Grüneisen parameter
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)

## Slide 15
Effect of nano-structuring on thermal conductivity
By reducing grain size thermal conductivity can be reduced by 30 %
Grain Size 100-5000 nm for CdSb and 100-1000 nm for ACd2Sb2
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)

## Slide 16
Figure of merit
Large anharmonicity leads to high ZT (1.9)
Comparable to the other state of the art Zintl thermoelectric materials
Nature Materials 7, 105 - 114 (2008)
1 Chem. Mater., 2015, 27 (3)
p-type
n-type
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)

## Slide 17
Conclusions
Heavy and light combination of bands leads to large power factor
Strong anharmonicity results in low thermal conductivity
By changing cation layer thermal conductivity can be reduced
ZT is comparable to best know thermoelectrics
Indian Institute of Science, Bangalore
Phys. Chem. Chem. Phys.17, 16917 (2015)

## Slide 18
  Breaking the inverse coupled dependence of S and σ
Indian Institute of Science, Bangalore

## Slide 19
Bi2S3: Possible good thermoelectric material
Moderate 1.23 eV band gap semiconductor
Large thermopower and low thermal conductivity
Poor electrical conductivity
For Bi2Te3: ZT ~ 1.5
Data from: Adv. Energy Mater. 2012, 2, 634–638
1. Solid State Communications 162 (2013) 48–52
2. Journal of Alloys and Compounds 514 (2012) 205– 209
Current scenario for Bi2S3
Pressure can be used to improve σ
Indian Institute of Science, Bangalore

## Slide 20
How pressure can tune thermoelectric properties?
High density of states effective mass (m*dos)
Low conductivity effective mass (m*cond)
Phys. Rev. Applied 3.064003
Condition for high S and σ
Density of states effective mass
At a fixed T and carrier conc. (n)
Conductivity effective mass
Indian Institute of Science, Bangalore

## Slide 21
How pressure can tune thermoelectric properties?
Tuning of band gap and band dispersion
Due to reduction in either S or σ, pressure induced tuning is not very significant
Careful band structure engineering can lead to high ZT
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)
Notes: The first figure denotes the inverse coupled dependence of S and sigma with pressure. As S increases sigma starts to decrease. The opposite is also true. hence although the enhancement is observed but it is not very significant. The second figure shows the condition for simultaneous enhancement of S and sigma. If band structure can be tuned in such a way that m_cond decreases with pressure and m_dos increases with pressure this will lead to Simultaneous enhancement in S and sigma leading to huge power factora as shown in figure 3. this is what we have shown for Bi2S3.

## Slide 22: Electronic structure under pressure
Hydrostatic pressure significantly modifies the conduction band
Compression indicates anisotropy in crystal structure
Semi conductor to metal transition at 17.3 GPa
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)

## Slide 23: Carrier effective mass
m*cond decreases with pressure
m*dos increases with pressure for n-type
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)

## Slide 24: Transport properties under pressure
Simultaneous enhancement of S and σ under pressure for n-type doping
Five fold enhancement in power factor under pressure
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)

## Slide 25: Effect of pressure on thermal transport
According to Liebfried and Schlömann theory
Very low lying optical modes
Strong overlap between acoustic and optical phonons
Optical modes split under pressure
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)

## Slide 26: Thermal conductivity under pressure
Nominal change in thermal conductivity in the pressure range of interest
(P ≤ 0 ≤ 7.5 Gpa)
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)

## Slide 27: Figure of merit
Very small change in relaxation time
ZT ~ 1.2 for n-doped Bi2S3
ZT ~ 1.0 for p-doped Bi2S3
Indian Institute of Science, Bangalore
J. Mater. Chem. C, 4, 1979 (2016)
Notes: Deformation potential theory black dot sigma/tau compare it with the experimeent

## Slide 28: Effect of equivalent chemical pressure introduced by doping
Doping results in 3 GPa chemical pressure
Softening of phonon modes upon doping
Band gap reduces upon Sb doping
Bi
Sb
S
J. Mater. Chem. C. 4, 1979-1987 (2016)

## Slide 29: Effect of equivalent chemical pressure introduced by doping
Enhancement in power factor upon doping
Reduction in lattice thermal conductivity upon doping
J. Mater. Chem. C. 4, 1979-1987 (2016)

## Slide 30
Reversible tuning of band gap of Bi2S3 using hydrostatic pressure semiconductor to metal transition at 17.2 GPa
m*cond decreases and m*dos increases with pressure for n-type
Weak dependence of thermopower at low pressures for p-doped Bi2S3
Simultaneous enhancement of S and σ for n-doped Bi2S3
Thermal conductivity shows nominal increase at low pressures
Large ZT of 1.2 and 1.0 for n and p-doped Bi2S3, respectively
Conclusions

## Slide 31: Future direction
Indian Institute of Science, Bangalore
High throughput screening of thermoelectric materials
Phys. Rev. B 92, 085205 (2015)
Band Engineering in Semiconductor
PRL 114, 136601 (2015)
From lab to industry
The Electrochemical Society Interface • Fall 2008

## Slide 32: Before and after SahasraT

## Slide 33: Publications using SahasraT
11 publications after the establishment of SahasraT

## Slide 34: Happy birthday SahasraT!

## Slide 35
Thank You